Inland TW Vacuum Pump Oil 

Description:
Inland TW® is a semi-synthetic hydrocarbon vacuum oil specifically recommended for applications in rotary vane pumps where exposure to reactive or corrosive gases is prevalent. This product is a distilled hydrocarbon containing no additives. Both unsaturates and aromatics have been removed, resulting in a superior, longer-lasting pump fluid.

Inland HVTW® is also available for use in piston pumps, with the appropriate viscosity necessary. Typical applications include nitride deposition, LPCVD, plasma etching, and ion implantation. When compared to Invoil 20, Inland TW lasts 1.5 to 4 times longer.

Beneficial Features:
  Longest lasting hydrocarbon 
  Corrosion resistant 
  Low vapor pressure 
  USP grade


	Specification
	Inland TW

	Vapor Pressure @ 25 °C: 
	<1 x 10-6 torr

	Boiling Point @ .01 torr: 
	158 °C (316 °F)

	Viscosity @ 40 °C: 
	56 cst (260 SUS)

	Viscosity @ 100 °C: 
	8.9 cst (55.4 SUS)

	Pour Point: 
	-12 °C (10 °F)

	Flash Point: 
	243 °C (470 °F)

	Fire Point: 
	270 °C (517 °F)

	Density: 
	0.86 g/cc




Vacuum Applications:
  Nitride deposition 
  LPCVD 
  Plasma Etching 
  Ion implantation 
  Other corrosive applications


